Dubsil 22

Processing:

- Gently shake each of the two components (part A and B) every time before using

- Add 1 part of part A to 1 part of part B.

- Mix thoroughly in a clean vessel until a homogeneous colour is obtained

Mix gently in order to avoid air bubbles from being entrapped

- Pour into flask

- Remove from flask after material has cured (approx. 45min)

- When pouring stone into silicone mould a wetting agent is recommended

Warning: for mixing use only clean stainless steel or plastic vessels.