### MONOCURE PLATEBOND 30ML

### APPLICATION & TIPS

Ensure the build plate is clean and dry. Apply a few drops onto your 3D printer's build plate using the dripper provided.

Using a metal scraper or gloved finger, smear the PLATEBOND™ liquid UV adhesive across the entire print area.

Allow the 3D printer to cure the PLATEBOND™ with the first few base layers. (It does not need to be cured before printing).

If the model is difficult to remove after printing, run hot water over the back of the build plate to help release the 3D printed part(s).

### HOW TO HANDLE PLATEBOND

Storage
Store PLATEBOND™ in a dry, cool place, away from direct sunlight.

Warning
This is a UV sensitive product. Please keep the lid on when not in use.

PPE
Always wear recommended safety PPE when handling this product.

### PHYSICAL PROPERTIES

Product Code(s)  3DPB-3793

Colour(s) Transparent

Viscosity 1000cps

Odour Negligible Characteristics

Shelf Life 36 months

Active Solids 100%

UV Cure 225nm to 420nm

Cure Speed Very fast with UV Lasers & LEDs

Storage Dark Cool, dry place out of direct sunlight.

Wash Up RESINAWAY® or IPA (Isopropyl Alcohol)